## Slide 1: 12 GHz Si3N4 Microresonator: Characterization
Chip number: D63_3_12GHz_F4_C12
In the range around 1542 nm
Total linewidth /2  20 MHz
Intrinsic linewidth 0 /2  8 MHz

## Slide 2: 12 GHz Si3N4 Microresonator: soliton generation
All the resonances around 1542 nm can generate multi/single soliton with
pump power above 400 mW (i.e. on chip power above 200 mW)
p=1542.0 nm
Pin=400 mW
p=1542.3 nm
Pin=400 mW