## Slide 1
Saturation regime.
As the signal increases in power, the gain decreases since the pump cannot longer replenish the inversion as fast as the signal depletes it. (Depopulation of excited state due to an increasing number of signal photons)
Why saturation regime brings down ASE?
There is an interplace. In this regime, more seed does not have higher amplification but, also, there is a very few amount of residual inversion that ASE can catch up.
If the seed is weak, the ASE can collect a large amount of the inversion
Operation outside saturation allows more ions to be used for amplification (higher efficiency) but also, more ions are available for be taken by ASE (Higher noise)
Why SNR increases with input power?
Inversion is mostly taken by the input signal and does not leave inversion available for ASE generation

## Slide 2
Noise figure
Why do we want low noise at the beginning of the amplifier?
The first amplifier has the most significant effect given the noise figures of the following stages are reduced by stage gains.
The first amplifier should have a low noise figure, and the noise figure requirements of subsequent stages can be more relaxed.
The highest inversion gives the smaller value. .
Negligible population of the ground level prevents reabsorption of the signal
Noise output power in the bandwidth around the frequency where the gain of the amplifier is G
Increases with gain and low inversion.
It is reduced with high inversion

## Slide 3
Why not operate with 5 dB/m gain fiber?
Case 1: We want to get a gain of 5 dB  We need more than 3 m of fiber (When for 22 dB/m fiber ~ 0.5 m)
    Higher pump powers are now required at the input to invert the entire fiber, especially towards the end of the fiber.
    Such amount of high power plus longer fiber generates a larger amount of ASE
    The ASE increases exponentially with length: with increasing ﬁber length, the values of generated noise will be increased due to the accumulation of previous noise
Case 2: Short fiber (0.5 m) of 5 dB/m gain. The output gain is less than 1 dB. Forcing the second amplifier to provide the rest needed gain.
Why not operate with 80 dB/m gain fiber?
Too much erbium can be too much of a good thing because of clustering and cooperative up-conversion quenching of the excited state. Clusters: two ions close together that only absorb and no emission  If one ion absorbs, it is excited. If the second is also excited they exchange energy, exciting one of the ions to a higher stage and the other one falls to the ground state.

## Slide 4
Why not operate with 5 dB/m gain fiber?
Case 1: Long fiber, higher gain Case 2: Short fiber, lower gain
ASE increases up to 6 µW for a 280 µW output power ASE is kept low but signal amplification reach less than 120 µW

## Slide 5
Why do we want a short fiber?
  Shorter fiber prevents the growth of ASE (exponential dependence with length)
  But lower gain is available.
  A shorter fiber can be well inverted across its entire length, thus offering a good noise figure.
  However, a significant amount of pump light exits the fiber.
L = 2.5 m
L = 0.5 m
L = 1.5 m

## Slide 6: With all this in mind…
Multistage amplifier
ASE to be eliminated at the middle point along the fiber amplifier.
It is difficult to obtain simultaneously large gains and very low noise figures in a single stage amplifier.
By reducing the ASE, more gain is available for the signal and less noise is added to it from the spontaneous emission
The first stage needs to be well inverted so that a moderate amout of gain is obtained with minimal noise added.
PM isolator to be placed at the output of every stage to get rid of one polarization mode from ASE  reducition up to 50% the overall noise.
1st amplifier
  Fiber length = Short fiber. To be optimized
  Pumping power = Saturation regime
  Pumping direction = Forward although given the short fiber might be irrelevant
  Gain of active fiber = 22 dB/m
  Gain ~ 5dB
2nd amplifier
  Fiber = Longer fiber for higher gain. To be optimized
  Pumping power = Outside small signal gain
  Direction = Backward for higher efficiency and relaxed noise requirements
  Gain of active fiber = 27 dB/m for higher gain
  Gain > 15 dB

## Slide 7
Optimization fiber amplifier stages
24 dB – 27 dB
5 dB – 24 dB

## Slide 8: 1st amplifier
Operating in saturation regime. Low ASE respect to signal but low efficiency.

## Slide 9: 2nd amplifier
Not in saturation regime. Higher ASE respect to signal but higher amplification of the signal.

## Slide 10: 1st amplifier
Pump power = 120 mW
Output power = 300 µW
Pump power = 20 mW
Output power = 261 µW

## Slide 11: 2nd amplifier
Pump power = 100 mW
Output power = 14.5 mW
Pump power = 350 mW
Output power = 21 mW

## Slide 12
Final design
seed: output 1st stage
1550 fc/apc
1550 fc/apc
WDM
fc/apc 980
WDM
ISO*
ISO
fc/apc 980
seed: output microcomb
LD Pump2
Pµmo
Backward pumping
Forward pumping
LD Pump1
ISO
To input 2nd stage
24 dB/m, Er3+
0.5 m
27 dB/m, Er3+
1.9 m
*due to residual forward pump and backward pump from each amplifier respectively, this isolator might suffer some heat dissipation but, given the power values, should not be an issue.
~ 50 mW
~ 250 mW

## Slide 13
Some definitions…
The highest inversion gives the smaller value. .
Negligible population of the ground level prevents reabsorption of the signal
ASE
Independent from the photon number
Abs.
Stim.
photon flux density
abs. and emission rate
Photon density in the mode :
ASE power evolution
across a fiber
Noise output power in the bandwidth around the frequency where the gain of the amplifier is G
Increases with gain and low inversion.
It is reduced with high inversion